+

# TS/MME-MM

Section de Métallurgie et Métrologie/ Metallurgy and Metrology section

| Domaine / Field: LHC (Cold Mass) |  | Date: 27/03/2006 |  | N° EDMS / EDMS Nr.: 706247 |
| --- | --- | --- | --- | --- |
| Requérant / Customer: F. Savary AT/MAS | Liste de distribution / Distribution list: P. Fessia AT/MAS |  |  |  |
| Inclusion content of leaking collars |  |  |  |  |
| ## 1. Résumé / Abstract: Following leak testing of Cold Masses (CM), 10-5 mbar.l.s-1 leaks have been found on bellow collars. 3 welded assemblies have been brought for metallurgical inspection see ATTACHMENT 1 Material certificate has been provided and showed inclusion rating within CERN specification n° 1000 Ed.3 08/1999. This report contains the results of dye Penetrant Testing (PT) followed by micro-optical observations performed at the location of marked areas from previous tests at CMA (CM 2214) or issued from PT defect indications ( CM 2253 and CM 2264). |  |  |  |  |
| ## 2. Données expérimentales / Experimental data: 3 leaking welded assemblies containing bellow collars extracted from: CM 2214 (leaking area marked on the sample) CM 2253 and CM 2264 (no mark of leaking area) PT: P. Deweulf TS/MME/MM Micro-optical observations: QUANTIMET 600 Progressive polishing over 1 mm in the marked area for sample CM 2214 and polishing locally across the PT indications (see § 3) for samples CM 2253 and CM 2264 |  |  |  |  |
| ## 3. Résultats / Results: PT performed at CERN showed: No particular point has been detected for CM 2214 see ATTACHMENT 1 The presence of one particular point for CM 2253 and CM 2264. see ATTACHMENT 1 Micro-optical observations revealed the presence of one B type inclusion (aluminates) up to class 1 detected for sample CM 2253 and D type inclusion (oxides) up to class 1 for the three samples. Grain sizes (G = 4.5 for sample CM 2214 and G = 5.5 for samples CM 2253 and CM 2264) are below the maximum specified for 316LN see ATTACHMENT 2 Micro-optical observations of 1 mm further polishing performed across the identified area of sample CM 2214 did not show any visible leak path. The presence of inclusions of type D (oxides) up to class 1 is confirmed see ATTACHMENT 3 |  |  |  |  |
| ## 4. Discussion et conclusions / Discussion and conclusion: In conclusion, micro-optical observations only revealed the presence of D type inclusions (oxides) up to class 1and B type inclusions (aluminates) up to class 1 for sample CM 2253, which is below maximum specified in CERN specification 1000 Ed. 3 (maximum quoted at 1 for A, B C and 1½ for D type inclusions). No visible leak paths could be identified for the three samples. |  |  |  |  |
| ## 5. Annexes et références / Attachements and references: ## -ATTACHMENT 1: Visual observations + PT -ATTACHMENT 2: Micro-optical observations samples CM 2214, CM 2253 and CM 2264 -ATTACHMENT 3: Micro-optical observations samples CM 2214 (1 mm further polishing) |  |  |  |  |
| Redaction / Written by: A.Gerardin /TS/MME/MM |  |  | Approuvé par / Accepted by: S. Sgobba/TS/MME/MM |  |
| Expériences / Testing by: A.Gerardin/ P. Deweulf /TS/MME/MM |  |  | Superviseur / Supervisor: S. Sgobba/TS/MME/MM |  |

Rapport expérimental / Investigation report

### ATTACHMENT 1:

Visual observations of the collars:

Area of detected leak

Polishing direction

CM 2214

Penetrant testing:

Particular point

CM 2253

CM 2264

Particular point

### ATTACHMENT 2:

Micro-optical observations, original magnification: 100 x:

Sample CM 2214:

Average grain size number G = 4.5

Sample CM 2253:

B type up to class 1

Average grain size number G = 5.5

Sample CM 2264:

Average grain size number G = 5.5

### ATTACHMENT 3:

Micro-optical observations of sample CM 2214, after polishing 1 mm further:

Original magnification: 100 x, D type inclusion up to class 1