| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza – F. Terzi | 5. Date: 20/03/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBA_A001-02000014 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

X-ray test of longitudinal welds W1 & W2 of shrinking cylinders on CM nr.2014, showed defects as described on test reports Ansaldo-SIGE nr. 03052-52 & 53. Reports & films have been submitted to CERN analysis on 25/03/2003. ASG and CERN agreeded to proceed with n.9 repairs on W1 & n.20 repairs on W2. After these repairs (1st repair), X-ray test report nr. 03052-70 & 72 showed n.2 defects on W1 & n.3 defects on W2, in agreement with CERN analysis. ASG proceeded with 2nd repair: X-ray test report nr. 03052-76 showed no defects.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) On the 13th of May 2003, CERN Project Engineer has examined the radiographs of the repair-welds, W1 R and W2 R. W1 R shall be repaired according to the inspection report of SIGE, document under ref. 03052-70 dated 06-05-03. W2 R, defects on sections 5-6 and 34-35 can be left “as is”. This must be done under Ansaldo responsibility. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: 28 May 2003 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 29/05/2003 | Name: Date: |