| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B. Caserza | 5. Date: 12/05/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A001-02000024 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMB__A0001/G (620RM08234/L) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During discharge test at 3 kV on c.c. 2024, a short circuit occurred between poles nr. 02P30096 and 02P00097 (aperture D2) at 1610 mm from CS end: according to CERN, we proceeded with de-collaring of about 3m of collared coils from CS. The damage has been caused by a non-ferrous inclusion between the two poles: the SC cables has not been damaged. Then we proceeded with restoring the insulation between the poles. Damage and restored insulation has been shown to CERN personell (Mr. Musso) on 13/05/2003. All necessary electrical test will be performed after re-collaring.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - Repair ground insulation as said above, redo the assembly of the collar packs and the collaring operation. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: 13/05/03 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F.Terzi Date: 13/05/03 | Name: Date: |