| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza – F. Terzi | 5. Date: 28/10/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: Pole 02P00259 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMB__A0010/D (620RM08203/F) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection | Final inspection |
| In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During electrical test, with end under load, on pole 02P00259 (cold mass 2065), an anomalous L value has been detected. Then resistance measurement and discharge test showed a short circuit on CS between 6th and 7th turn of inner layer 02I00262 (SC cable 01B10279A). See annex photo for details. Note: critical current of SC cable Ic=538A (min. required Ic=491A) Pole is left pending, waiting for CERN inspection.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - The layer cannot be used in these conditions. It is definitely rejected (after visual inspection in ASG premises). |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: December 19th, 2003 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 22/12/2003 | Name: Date: |

Inner layer 02I00262