| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 19/01/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A001-02000064 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

X-ray test of longitudinal welds W1 & W2 of shrinking cylinders on CM nr.2064, showed defects as described on test reports Ansaldo-SIGE nr. 04052-221: no defects on W1 & nr.1 defect on W2. ASG will proceed with these repairs.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) Repair according to indications given in the above mentioned test report. Then, report on the final results. As far as we know, the welds of this cold mass have not been checked fully (please refer to e-mail of Mr. Drago dated December 16th, 2003 regarding priority cold masses). In order for us to trace back easily information, please add in this non-conformance report the position of the weld sections, which have been inspected (including the production test plates). |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: January 21st, 2004 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 26/01/2004 | Name: Date: |

CLOSURE OF THE NON CONFORMITY

Planned actions have been completed and corrective/preventive actions have been initiated (continuation page)

The inspected weld sections are:

a) L=500 mm (about) on CS and NCS test plates (both sides W1& W2)

b) L=1500 mm at both extremities of the CM: X-ray film id. = W1 & W2 pos.1 to 4;   W1 & W2 pos.35 to 39)

c) L= 800 mm on W1, in the central part of the CM, from 5000 mm to 5800 mm from CS: X-ray film id. = W1R & W1R1

Test report about  the final results will be annexed to the Traveller, as usual

F. Terzi