| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 27/09/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A054 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 510 pcs. |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: LHCMB__A0054 |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

The following Cu wedges, listed in the next page, showed hard oxidations. See also annexed photos for details Outokumpu production date: 23/01/2004 and others. SELVA tried to remove these oxidations without any results, so, at the moment, the material is in "stand-by". CERN checked the material in ASG on July.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) ASG, in agreement with CERN, rejected these material. The material will be sent to CERN for replacement. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: | Date: |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |

IDENTIFICATION

a) List of oxidated Cu wedges:

| Batch Nr. | Profile type | Pcs. |
| --- | --- | --- |
| 52 | I | 4 |
| 60 | III | 18 |
| 67 | III | 24 |
| 68 | I | 20 |
| 69 | II | 7 |
| 74 | I | 160 |
|  | II | 21 |
|  | IV | 27 |
| 75 | I | 35 |
|  | II | 168 |
|  | IV | 106 |

b) summary about the type of Cu-wedges:

Total number:

- type I	: 219 pcs.

- type II	: 196 pcs.

- type III	:   42 pcs.

- type IV	: 133 pcs.

1/3

2/3

3/3

1/5 2/5

3/5 4/5

5/5