| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 13/05/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A133 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

Yoke laminations (batch nr EYA00100 - EYA00101 - EYA00102) received at Ormet, showed dirty surfaces (see annexed photos). At the moment, the material is in "stand-by". Mr. Musso and Mr. Heer checked the material at Ormet and took away a lamination for visual inspection at CERN. ASG is asking CERN to check the material and take a decisione about it.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) The yoke laminations can be used as is. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary) We will complain to CERN supplier so that this does not happen anymore in the future (Action: CERN).

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F. Savary | Date: June 14th, 2004 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 15/06/2004 | Name: Date: |

IDENTIFICATION

10. Description of non conformity (continuation page)

1/2

2/2