| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza, F. Terzi | 5. Date: 11/10/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBBLA001-02000114 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: 683RM08450/B |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During final electrical test performed at 1.5 kV on CM 2114, a low insulation resistance value has been detected between Bus Aux.+Spools and ground (bus nr. 18 & 19): measured value R=0.1 MOhm at 0.1 kV (nom. R>1000 MOhm at 1.5 kV) In order to find out the cause of the problem, we disconnected aux. bus-bars nr. 17 & 20. A carefull check of all the connections, showed low insulation resistance between spool aux. bus-bars (bus nr. 19/20 and V-Tap EE931) and ground Spool id. nr. MCS-MA-E0102 installed on Apt.2

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) ASG propose to cut the weld of the capillary tube to detect exactly where is the weak point? This was done and it turned out that the problem is rather linked to the sextupole magnet. Therefore, the end cover shall be cut off for further investigations (change the corrector magnet if it is indeed the cause of the problem). CERN wants to be present during the execution of the tests after the end cover removal. ASG to notify CERN in due time for the travel organization. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F. Savary | Date: October 14th, 2004 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 15/09/2004 | Name: Date: |