| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza, F. Terzi | 5. Date: 28/10/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBALA001-02000117 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: 683RM08450/B |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During electrical test at 1.5 kV, performed before welding of end covers on CM 2117, a low insulation resistance to ground has been measured on different corrector magnets id nr. MCS-MA-E0297; MCS-MA-E0298; MCDO-MA-E0028 Measured leakage current: I=13μA (nom. value 2μA) Corrector magnet has been disinstalled from CM and tested again: the following values of leakage current have been foiund: - I=13.3 μA on MCS-MA-E0297 - I=8.6 μA on MCS-MA- E0298 - I=6.05 μA on MCDO-MA-E0028

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) Corrector magnets dismantled from CM, will be sent to CERN for inspection. The following corrector magnets have been installed on CM 2117: MCS-MA-E0812; MCS-MA-E0901; MCDO-MA-E0138 id. nr. MCS-MA-E0709 |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary) The insulation problem seems to be linked to the high rate of humidity in the assembly hole. A visit of MEL was effectuated in ASG to verify the measuring procedures. The magnets will be tested at CERN. Actions from MEL side are under study.

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: Marta Bajko | Date: 01.11.2004 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |