| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 20/12/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A001-02000148 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: LHCMB__A0001/G (620RM08234/L) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection | Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

After collaring of CC 2148, electrical test showed a short circuit between QH YT211 (ASGCICO-B0572) and outer layer 02E00596 of pole 02P00593 (D2-lower).

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. | Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - ASG will proceed to open the C.C. and change all the necessary components (quench heaters, coils protection sheets, ground insulation, cold bore tubes). |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: Marta Bajko | Date: 06.01.2005 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated All the necessary components have been changed. CC 2148 has been re-collared and electrical test performed successfully. |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 10/01/2005 | Name: Date: |