| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 20/12/2004 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB_A001-02000140 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: HCDCBHA055 |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During electrical check of bus-bar nr. B-358 (id. nr. HCDCBHA056-BI000358), before welding of end covers on CM 2140, a low insulation resistance between bars has been found. Measured insulation resistance R=24M (nom. value R>1000 M) All the electrical tests performed before longitudinal welding were OK: measured insulation resistance better than 1000 M On 09/12/04 CERN personnel, Mr. Perinet-Marquet and Mr. Urpin, made an adjustments of the ends of the bus-bars. On 17/12/04 the electrical check showed low insulation resistance between bars: this problem has been checked also by CERN personnel, Mr. Perinet-Marquet and Mr. Urpin, during their visit in ASG on 17/12/04.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) ASG action is to flow the bus-bars with dry nitrogen and heat that bars with electrical current, waiting for an increasing of the insulation resistance. ASG is also waiting for an alternative proposal from CERN. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary) ASG should go ahead in case of good resistance after dry with nitrogen.

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: Marta Bajkoi | Date: 06.01.2005 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |  |
| --- | --- | --- | --- |
| 16 | Project Management: |  | Date: |
| CLOSURE OF THE NON CONFORMITY |  |  |  |
| Planned actions have been completed and corrective/preventive actions have been initiated Electrical test completed successfully: please refer to data file "CM_B_2140.xls" |  |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |  |
| 17 | Name: F. Terzi Date: 10/01/2005 | Name: Date: |  |