| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 21/07/2005 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A001-02000233 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: LHCMB__A0001/G (620RM08234/L) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection | Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

After collaring of CC 2233, electrical test showed a short circuit between QH YT222(+) (id. nr. CIV-01809) and outer layer 02E00935 of pole 02P00932 (D2-upper). We found the problem just after the collaring and with the c.c. still under the press we were able to localize where it was (180 mm from the C.S. on pole D2U). Then we removed the pins for about 700 mm and we went out. We found a very small metallic particle between q.h. and the turn 17th just at 180 mm from the C.S. We removed carefully the particle and verify the integrity of the insulation of the other turns closed to the 17th ; we put a piece of kapton in that region and recollared again. The electrical check done was ok.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. | Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. | Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: | Date: |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |