| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name:B.Caserza – F.Terzi – M.Bergamini | 5. Date: 08/11/2005 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A100 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: LHCMB__A0099 rev.C |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

A dimensional test on collars regarding different batches nr. MAL00423 – MAL00450 – MAL00708 - MAL00709 – MAL00712 – MAL00713 has been performed. We found non-conforming values about the planarity on both measuring conditions: "Free State" and "Restrained Condition" (CERN ref. dwg. LHCMB__A0100 rev. C). Measured values: planarity error 0.4 ÷ 0.8 mm. About batch nr. MAL00710, collars have been already assembled in packs by Brandi. Planarity of the packs is not very bad, so ASG will complete the packing and will try to install them on a collared coil.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - ASG propose to sent back to Malvestiti collars, regarding batches nr. MAL00423 – MAL00450 – MAL00708 - MAL00709 – MAL00712 – MAL00713, for correction. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: | Date: |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |