| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 25/01/2006 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: 02C91541D |
| 3. Contract No: F462/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: LHCMB__A0012/E (620RM8188/B) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During wrapping operation, at SELVA, of sc cable nr. 02C91541D for outer layer (CM 2325), the cross-section of the cable buckled along 1 m of length. This damage occurred because the Apical tape, 11 mm wide, broke during wrapping: SELVA personnel stopped wrapping immediately. Besides two arm of the wrapping machine broke.: SELVA had to change the damaged parts in order to continue wrapping operation.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework | Return to supplier |
| Description of proposed action (use continuation page if necessary) The cable will be sent back to ASG for visual inspection: then it will be sent to CERN. The defect apical spools will be at ASG on next Wednesday and it will be showed to Mr. Musso. ASG is asking CERN a replacement outer layer cable. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: | Date: |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |