| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 20/07/2006 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMB__A133- FSG00533 / FSG00552 / FSG00548 / FSG00546 / FSG00544 / FSG00543 / FSG00542 / FSG00539 |
| 3. Contract No: F462/LHC/LHC | 7. Qty: |
| 4. Project Engineer: F. Savary, M. Bajko | 8. Dwg No: |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

See description and pictures on continuation pages.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) We shall proceed as we did in the past, i.e. clean off the rust at the latest stage (from e-mail dated 28/04/2006 by Mr. F. Savary) This means that the laminations, not yet stacked, shall be assembled “as is” and the outer surfaces cleaned at the final stage of assembly at ASG works when the packs are put together to make the ½ yokes. All the lamination packs shall be cleaned in such a way the corrosion is totally removed from the visible/accessible surfaces (with Scotch-Brite and vacuum cleaning). |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: Marta Bajko | Date: 21.07.06 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |

IDENTIFICATION

10. Description of non conformity (continuation page)

Yoke laminations regarding different batches received at ORMET from FSG, showed oxidation on the punched surface. Bathes id nr.

HCMB__A133-

FSG00533 / FSG00552 / FSG00548  /  FSG00546   /  FSG00544 / FSG00543 / FSG00542  /  FSG00539

Please find here some pictures.

Fig.1/4 - FSG00548

Fig.2/4 - FSG00544

Fig.3/4 - FSG00546

Fig.4/4 - FSG00542