| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: F. Terzi | 5. Date: 27.11.2006 |
| 2. Contractor/Supplier: ASG Superconductors S.p.A. | 6. Part description: HCMB__A001-02000431 |
| 3. Contract No: F462/LHC/LHC Amendment n.4 | 7. Qty: 1 |
| 4. Project Engineer: M. Bajko | 8. Dwg No: LHCMB__A0012/E (620RM08201/F) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During winding of the last turn of inner layer nr. 02I01725 (sc cable nr. 01B11029E) for CM 2431, a malfunctioning of the winding machine Spirex 1500 caused a damage of the sc cable (see annexed picture on continuation page). This damage has been probably caused by a failure of the sensor of the tension of the cable.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) Inner layer 02I01725 shall be rejected. ASG is asking CERN a new inner layer cable on ASG expense. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary) the new cable id to be traced on this NCR.

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: Marta Bajko | Date: 29.11.2006 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |

1/4

2/4

3/4

4/4