|  | NON CONFORMITY REPORT | Nr. NC CERN 54 (CERN NC id. num.) |
| --- | --- | --- |
| Ansaldo Superconduttori S.p.A. |  |  |

| CUSTOMER CERN |  | JOB 0209EM |  | PROJECT NAME LHC 30 cold masses |  |  | Nr. RNC 020524A (ANSALDO NC id. num.) Date: 24/05/2002 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PRODUCT IDENTIFICATION Inner layer I061 |  |  |  |  |  |  |  MAJOR  minor |  |
| REFERENCE DOCUMENTS |  |  |  |  |  |  |  |  |
| NON CONFORMITY DESCRIPTION |  |  |  |  |  |  |  |  |
| After curing, inner layer nr. I061 (cable nr. 01B10073A) has air gap between Cu wedges and end spacers. In particular: - on C.S. gap=2.1mm between Cu wedge and end spacer pos.7 - on C.S. gap=1.9mm between Cu wedge and end spacer pos.13 - on N.C.S. gap=2.1mm between Cu wedge and end spacer pos.3 - on N.C.S. gap=2.3mm between Cu wedge and end spacer pos.4 Besides first turn on N.C.S. is detached along 200mm about This defect has been already showed to CERN people during visit at Ansaldo on 22/05/02. |  |  |  |  |  |  |  |  |
| We propose to fill in all the air gap using epoxy glass filler and to impregnate with Stycast. |  |  |  |  |  |  |  |  |
| INTERNAL APPROVAL |  |  |  |  |  |  |  |  |
|  | PREPARED |  | CHECKED |  |  |  |  | APPROVED |
| Dept. | PRC |  | TEC |  |  |  |  | TEC |
| Name | B. Caserza |  | G. Drago |  |  |  |  | F. Terzi |
| Signature |  |  |  |  |  |  |  |  |
| Date | 24/05/2002 |  | 24/05/2002 |  |  |  |  | 28/05/2002 |

| CORRECTIVE ACTIONS |  |  |  |
| --- | --- | --- | --- |
| CUSTOMER APPROVAL |  |  |  |
|  ACCEPTED, by F.Savary on the 18th of September 2002 |  |  NOT ACCEPTED |  |
| REMARKS |  |  |  |
| - Resolution already discussed and therefore applied in due time; - Resolution implemented under Ansaldo responsibility. |  |  |  |
| CORRECTIVE ACTION EXECUTED |  |  | REPORTS ISSUED |
| Date | Signature |  |  |
| REMARKS |  |  |  |

MOD NC-CERN_2