| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza | 5. Date: 17/09/2002 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBB_A001-02000004 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

After repairing of longitudinal weld WA on CM nr. HCMBB_A001-02000004, X ray examination showed a lack of fusion, about 60 mm long (ref. film pos. 26-27). Films delivered to CERN (Mrs. Bajko) on 09/10/2002. Reference documents: SIGE Test Reports 02052-3

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) Ansaldo shall repair the defective part of the weld and then, check it again according to the Technical Specification. Lack of fusion is a type of defect that is not acceptable. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary) CERN recommends Ansaldo to improve the working conditions during repairing, i.e. improve either welding parameters or geometry of the bevel that is made by removal of the defective part. Such repair welds shall be made according to a well-established welding procedure specification (WPS).

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: 18th Sep 2002 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated (*) |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 11/10/02 | Name: Date: |

NON CONFORMITY CONTINUATION PAGE

(*)

Repairs of repaired parts on WA weld executed on 05/10/02.

X-rays examination performed 07/10/02: no defects detected. Refer to SIGE test report nr. 02052-6 for details.

Check of X-ray films performed on 10/10/02 at ASG with Mr. Savary (CERN): weld repairs acceptable

ANSALDO SUPERCONDUTTORI

LHC Quality Assurance

F. Terzi