| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza | 5. Date: 13/01/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: pole P096 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMB__A0010/D (620RM08203/F) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection | Final inspection |
| In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

During discharge test performed on pole nr.P096, with end under load, a discharge occurred on CS end at 4.8 kV between 6th and 7th turns of inner layer nr.I099.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - After having inspected the damage, one strand of inner layer I099 broken as can be seen on the enclosed picture, on Thursday 16th January 2003 at Ansaldo premises (A.Musso and F.Savary together with Ansaldo staff), we decided, obviously, to reject the layer. - Ansaldo to cut out the head of the damaged layer so that CERN staff can bring it to Geneva for further investigation with cable experts and metallurgists. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary) Ansaldo to investigate what may have provoked such damage (eventually look at the tooling and various operations carried out at the previous stages of the coil’s manufacture).

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: 20th Jan 2003 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 13/01/2003 | Name: Date: |