| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B. Caserza | 5. Date: 10/12/2002 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBB_A001-02000009 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
| Incoming inspection | Final inspection |
| In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

Intermediate geometrical measurements (after longitudinal welding of the shrinking cylinder) performed on c.m. HCMBB_A001-02000009 showed an out-of- tolerance about the curvature. Please ref. to test report (midplane analysis) already sent Mrs. Bajko.

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - The curvature of the cold mass shall be put within the specified tolerances. Because CERN needs to investigate more in details the question of the long-term dimensional stability of a cold mass assembly, which may be affected by the operation of correction of the curvature, the procedure shall be precisely described and all measurements recorded in the traveller (for internal use at CERN: please refer to meeting report AT-MAS/FS 6880 dated 31st January 2003). - … See continuation page |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: 31st January 2003 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |

DISPOSITION Continuation of section 13

CERN staff will give additional recommendations to Ansaldo (action F.Savary and M.Bajko) on how to proceed (what to do, what to measure and what to record) for the correction of the cold mass. CERN staff will also follow carefully the execution of the corrective actions.