| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza | 5. Date: 18/10/2002 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBB_A001-02000012 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

see description on pag.2

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) Considering the successive repairs, which have been checked as described by AS in page 2 (level R3 on both welds), the two defects still present in WA, position 20-21, can remain and the weld should be left “as is”. Ansaldo Superconduttori S.p.A must take the responsibility of such an outcome. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: F.Savary | Date: 3rd of April 2003 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 03/04/2003 | Name: Date: |

NON CONFORMITY CONTINUATION PAGE

X-ray test of longitudinal welds WA & WB of shrinking cylinders on CM nr.2012, showed defects as described on test reports Ansaldo-SIGE nr. 02052-8 & 9.  After 1st repair, some other tests and repairs followed, according to Ansaldo-SIGE reports nr. 02052-15 & 16, 02052-17 & 18, 02052-22 & 23 and according to Ansaldo-CERN discussion.

All these reports and films have been submitted to CERN analysis.

At the end only 2 repairs were agreed to be done (seen with A.Costa during visit from 15th to 17th of January 2003, refer also to visit report AT-MAS/FS 6897)

Results of these repairs (4th time at the same positions nr. WA 20-21 & WB 2-3) are in Ansaldo-SIGE reports nr. 03052-28.

Weld WB 2-3 is OK. Weld WA 20-21 shows a lack of fusion of about 27 mm between 1st & 2nd pass and two lacks of fusion of 45 mm about between 3rd & 4th pass.

F. Terzi