| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza | 5. Date: 22/01/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBB_A001-02000007 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

see next page

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: on behalf of F. Savary, A.Musso | Date: 17/04/03 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F.Terzi Date: 17/04/03 | Name: Date: |

X-ray test of longitudinal welds W1 & W2 of shrinking cylinders on CM nr.2007, showed defects as described on test reports Ansaldo-SIGE nr. 03052-26 & 27.

Reports and films have been submitted to CERN analysis on 05/02/2003: ASG and CERN agreeded to proceed with n.2 repairs on W1 and n.7 repairs on W2.

After these repairs (1st repair), X-ray test report nr. 03052-37 showed n.1 defect on W1 and n.1 defect on W2.

ASG proceeded with repairs (2nd repair): X-ray test report nr. 03052-43 showed no defect on W1 and n.1 defect on W2.

In agreement with CERN, taking into account that a 3rd repair on the same position could give worst result, W2 weld can be accepted as it is.