| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza | 5. Date: 17/02/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBBRA001-02000012 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

Final geometrical measurements performed on c.m. HCMBB_A001-02000012 showed an out-of-tolerance about the positioning of end-cover on lyre side, after welding. Measured value of the centre of the end-cover is -1.45 mm on x-axis

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. |  Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. |  Use-as-is |  Repair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - The maximum acceptable error on the end cover positioning is 0.75mm. Therefore the end cover as it is not accepted. Further investigations shows that also the corrector magnets are misaligned with the same order of magnitude, as the error was committed during the definition of the reference axes. - The end cover should be cut and repositioned as well as the corrector magnet. We suggest making the cut of the end cover in the welded zone in such a way to save the correct overall length of the magnet. Than perform an eccentric machining in order to correct the horizontal misalignment mentioned here before. The machining can be made at a bigger diameter than specified and the gap between the cylinder and the transition ring corrected with stainless steel shim. The end cover could be re-used on a different magnet by taking into account its short length, which can be compensated by the length of the cylinder. |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: Marta Bajko | Date: 11.02.2003 |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: F. Terzi Date: 02/03/2003 | Name: Date: |