| – |
| --- |
| Non conformity Report |  |
| IDENTIFICATION |  |
| 1. Originator’s Name: B.Caserza | 5. Date: 20/03/2003 |
| 2. Contractor/Supplier: Ansaldo Superconduttori S.p.A. | 6. Part description: HCMBBRA001-02000008 |
| 3. Contract No: F302/LHC/LHC | 7. Qty: 1 |
| 4. Project Engineer: F. Savary | 8. Dwg No: LHCMBB_A0002/F (683RM08451) |

| 9. Found during what activity: |  |
| --- | --- |
|  Incoming inspection |  Final inspection |
|  In-process inspection |  Other: |

10. Description of non conformity (use continuation page if necessary)

Final geometrical measurements performed on c.m. 2008 showed: - out-of-tolerance about the positioning of the cold feet pads after welding: measured values of distance between feet and midplane are 293.30 mm on CS and 293.49 mm on LS (nom. value = 294.00 ±0.5 mm.) - out-of-tolerance about outer diameter of the flanges on CS on V1 (d=75.72mm) and V2 (d=75.78mm): nom. value = 76mm -0.05/-0.15 - out-of-tolerance about outer diameter of the flanges on LS on V1 (d=73.33mm) and V2 (d=73.29mm): nom. value = 73.5mm -0.05/-0.15

11. Action taken to prevent misuse (use continuation page if necessary)

| IMPORTANCE |  |  |
| --- | --- | --- |
| 12. | X Non critical |  Critical |

| DISPOSITION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 13. | X Use-as-is |  XRepair |  Reject |  Rework |  Return to supplier |
| Description of proposed action (use continuation page if necessary) - Use a shim of 0.5mm on the 3 cold feet pads in order to correct the distance between the cold feet pads and the mid plane of the cold mass. - According to the new-relaxed tolerances the diameter of the flanges are acceptable up to 76mm-0.05/-0.025 on Cs and 73.5mm-0.05/-0.25 on LS. The flange V1 on CS of a diameter of 75.72mm still out of the relaxed tolerances should be repaired at CERN at the RECEPTION. - Th |  |  |  |  |  |

CORRECTIVE/PREVENTIVE ACTION

14. Description of proposed action (use continuation page if necessary)

| APPROVAL OF NON CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 15 | Project Engineer: | Date: |

| APPROVAL OF CRITICAL NON CONFORMITIES |  |  |
| --- | --- | --- |
| 16 | Project Management: | Date: |

| CLOSURE OF THE NON CONFORMITY |  |  |
| --- | --- | --- |
| Planned actions have been completed and corrective/preventive actions have been initiated |  |  |
|  | For non critical non conformities Quality Manager or Project Engineer | For critical non conformities Project Engineer |
| 17 | Name: Date: | Name: Date: |