+

Questions and answers

- Are curved shells more difficult to measure than the straight ones?

Yes, geometrical measurements on curved shells are more difficult than on straight shells because the shell has to be rotated of 90° before measurements. This is for inverting the vertical plane with the horizontal one.

- Do you have to go back to the welding press in case of bad curvature?

No, shells can be re-shaped without press. We have to remember that the geometry depends also from the supporting conditions.

- Is it not better to give the right shape by the geometry of the shells at room temperature in such way to avoid stress in cold conditions?

We tried to hammer the shells made in the welding press to release the stress in the shells. But this destroyed the geometry. We have to consider that stress can also be induced in shells having the right geometry at room temperature during transportation. Luckily the stress is redistributed during thermal cycles and in case of quenches in any of the two solutions. Therefore, these are equivalent.

###### Comments

Half shells could be produced of the so-called straight shells type, which are already naturally convex. This should be less expensive that producing curved shells and they would be easier to produce.