Insulation of cold bore tubes

D. Tommasini

Specifications

| Material of tube | AISI 316 LN |
| --- | --- |
| Max external diameter without insulation | 53.0(0.15 mm |
| External diameter with insulation | 54.20(0.20 mm |
| Surface | smooth |
| Adhesion strength of external wrap | > 20 g/mm |
| Test voltage | 6 kV for 5 minutes |
| Resistance to radiations | > 106 Gy |
| Resistance to thermal shocks | from 0 to 450 K |

Experiments done

| epoxy resin | normal / fast curing types | fast curing OK |
| --- | --- | --- |
| tape width | 30 mm, 20 mm | 20 mm OK |
| curing | shrinkable tape, 20-25-30 mm | 30 mm OK |
| pre-preg types | cloth / fleece | better a cloth |
| PI glue | inner/outer wrap | OK for outer |
| thermal shocks | from LN2 and also from He | OK |
| radiations | under test by Tavlet | OK on paper |

Materials

| First layer & second layers |
| --- |
| Type | Two wraps of polyimide tape epoxy coated, thickness 70(m including the glue. |
| Coating | ISOLA KREMPEL ISOVOLTA GTS |

| Third layer |
| --- |
| Type | One wrap of fast curing pre-preg tape |
| Product | SSY00C1 by ISOLA Isopreg HR200P37 by ISOVOLTA KREMPEL GTS |

| Fourth layer (overlapped) |
| --- |
| Type | Two wraps (overlapped) of polyimide tape coated with polyimide glue |
| Product | PIXEO AST252 by KANEKA |

Status and next actions

Materials

- In house for about 100 tubes.

- Qualification mid-February.

Procedures

- Specification mid-January.

- Demonstration wrapping for magnet makers end of January.

Strategy

- CERN procures the polyimides, including epoxy coated polyimides.

- The magnet maker procures the pre-preg, selecting one type among the ones qualified by CERN.