# Davide Tommasini

# Experiments on short models

Questions and answers

-What is the distribution of prestress inside the coils?

The coil prestress is reasonably the same from the collar nose to the mid-plane when the magnet is not excited. When the magnet is excited the magnetic field increases the prestress in the median plane and decreases it in the polar plane. Typical values are 20 MPa for the inner layers and 30 MPa for the outer layers.

# Text boxes

Pre-stress and field quality

- Pre-stress and training

- Sensitivity of magnetic field harmonics

- Conclusion

Conclusions

 High pre-stress loss between ambient temperature and cold

 The straight section is robust within a wide pre-stress range

(50-70 MPa for the inner layer ; 65 - 95 MPa for the outer layer)

 The sensitivity to coil size is close to the one estimated with ROXIE