Comments

We have left a certain degree of flexibility to the manufacturers concerning this operation during the series production. We will ask them for the price of a complete check per unit, and for checking the longitudinal and circular welds separately. The stress in circular welds is half with respect to the longitudinal welds; therefore the risk of defects is mush less.  We are considering the idea of not checking the circular welds at all.

Questions and answers

- Why don’t you use the eddy current method for detecting defects in the welds?

Because the eddy current method gives information about the presence of defects but not about their type.

- Do you plan to check the entire series production?

At the beginning, we will strictly check the production. Later, if the welding procedure will be respected, we will do only spot checks.