## Slide 1: Performance requirements for IR magnets Gijs de Rijk CERN

## Slide 2: Content
IR quad Magnet specification
Acceptance criteria
  LHC lessons
  Upgrade IR quads performance requirements

## Slide 3: IT quadrupole preliminary specification (Aug 2010)
Aperture A = 120 mm – 150 mm (t)
Gradient G = 175 T/m – 140 T/m (t)
Cold mass length 8 m – 10 m (t)
Maximum cold mass outer diameter = 600 mm (s)
Operation temperature 1.9 K (option 4.4 K) (t)
Operational current ≤ 13 kA (s)
Angular straightness (tilt) 1 mrad rms
Radiation hardness for (e) (with shielding):
  50 MGy
  2.1016 protons/cm2
  3.1018 neutrons/cm2
Maximum heat load
  Local 15 mW/cm3 in 10 cm length parts
  Global 50 W/m
Cold mass pressure tested at 26 bars (NB: t = tbd later, s = soft, e = estimate)

## Slide 4: IT quadrupole: acceptance criteria (Aug 2010) as derived from LHC
Acceptance criteria: (what do we call success ?)
  < 3 quenches to reach nominal gradient
    With more a series production will be problemetic
  < 10 quenches to reach 110% of nominal gradient
    We need to aim higher to be sure of the quality of the magnet at nominal
  Maximum 1 quench after thermal cycle to reach nominal gradient
    This is not really well know

## Slide 5: Quench performance: look back at LHC dipoles (1)
LHC dipoles reached nominal (87%) within 3 quenches

## Slide 6: Quench performance: look back at LHC dipoles (2)
The ultimate was reached within 8 quenches

## Slide 7: Quench performance: look back at LHC dipoles (3)
After 1 thermal cycle nominal was reached within 1 quench

## Slide 8: HQ: Training quenches
HQ training quenches:
Nominal = 80% ss = 156 T/m
Training Q in % ss
Training Q peak field
Training Quenches: Gradient

## Slide 9: HQ: high ramp rate quenches
The LHC quads will ramp around 15 A/s and down ~3x faster. During these ramps magnet are not allowed to quench: For HQ this is for some versions on the limit

## Slide 10: LQS01 Test at Fermilab (see G. Chlachidze’s talk)
LQS01b, a reassembly of LQS01a with more uniform and higher pre-stress, was tested in July 2010
  Reached 222 T/m at 4.6 K
LQS01b quench history

## Slide 11: LQS02 Quench History
Exceeded 200 T/m at 1.9 K and 2.6 K (only for ramp rates of 100-150 A/s) but failed to reproduce LQS01b performance

## Slide 12: IT quadrupole: acceptance criteria “revisited”
  ≤ 3 quenches to reach nominal gradient => 160 T/m (120 mm)
    The latest HQs show that this should be possible
  < 10 quenches to reach 110% of nominal gradient => 176 T/m
    The latest HQs show that this should be possible
  Maximum 1 quench after thermal cycle to reach nominal gradient
    This is not really well know