Attention please! Aperture no. 199 was build with 0,95 mm protection sheets, so the b6 value of this aperture can not be compared with other apertures listed in this report.

Cn (mT@12.5A)                3.773        3.769            3.772

# Mean value along the length of the aperture :  µ = 1.014

Pole pieces charge 59 = no measurement

Fixed flange = 1.05µ

End flange = 1.04µ