Cn (mT@12.5A)                3763             3762            3763

# Mean value along the length of the aperture :  µ = 1.005

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 94 = 1.007µ

Fixed flange = 1.08µ

End flange = 1.002µ