Cn (mT@12.5A)                3.755             3.754            3.753

# Mean value along the length of the aperture :  µ = 1.007

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 95 = 1.002µ

Fixed flange = 1.027µ

End flange = 1.003µ