Cn (mT@12.5A)                3.780             3.782            3.779

# Mean value along the length of the aperture :  µ = 1.017

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 84 = 1.013µ

Fixed flange = 1.093µ

End flange = 1.004µ