Cn (mT@12.5A)                3.777             3.778            3.775

# Mean value along the length of the aperture :  µ = 1.0155

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 84 = 1.014µ

Fixed flange = 1.086µ

End flange = 1.004µ