Cn (mT@12.5A)                3.771             3.780            3.770

# Mean value along the length of the aperture :  µ = 1.015

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 84 = 1.014µ

Fixed flange = 1.096µ

End flange = 1.004µ