Cn (mT@12.5A)                3776            3785             3776

Mean value along the length of the aperture: ( = 1,009

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 84 = 1.019µ

Fixed flange = 1,091µ

End flange = 1.004µ