Cn (mT@12.5A)                3.774             3.782            3.781

# Mean value along the length of the aperture :  µ = 1.010

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 73 / 83 = 1.019µ

Fixed flange = 1.084µ

End flange = 1.004µ