Cn (mT@12.5A)                3.770             3.767            3.770

# Mean value along the length of the aperture :  µ = 1.018

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 97 = 1.003µ

Fixed flange = 1.105µ

End flange = 1.003µ