Cn (mT@12.5A)                3.759             3.756            3.758

# Mean value along the length of the aperture :  µ = 1.005

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 98 = 1.003µ

Fixed flange = 1.095µ

End flange = 1.003µ