Cn (mT@12.5A)                3.751             3.750            3.752

# Mean value along the length of the aperture :  µ = 1.003

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 102 = 1.003µ

Fixed flange = 1.1µ

End flange = 1.003µ