Cn (mT@12.5A)                3.785             3.782            3.785

# Mean value along the length of the aperture :  µ = 1.019

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 71/72 = 1.02µ

Fixed flange = 1.095µ

End flange = 1.005µ