Cn (mT@12.5A)                3.788             3.787            3.788

# Mean value along the length of the aperture :  µ = 1.018

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 73/74 = 1.02µ

Fixed flange = 1.098µ

End flange = 1.004µ