Cn (mT@12.5A)                3.782            3.777            3.791

# Mean value along the length of the aperture :  µ = 1.024

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 71/74 = 1.02µ

Fixed flange = 1.102µ

End flange = 1.004µ