Cn (mT@12.5A)                3.789            3.785            3.779

# Mean value along the length of the aperture :  µ = 1.027

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 103 = 1.004µ

Fixed flange = 1.095µ

End flange = 1.003µ