Cn (mT@12.5A)                3.760            3.758            3.758

# Mean value along the length of the aperture :  µ = 1.003

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 105 = 1.005µ

Fixed flange = 1.098µ

End flange = 1.002µ