Cn (mT@12.5A)                3.767            3.765            3.766

# Mean value along the length of the aperture :  µ = 1.006

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 106 = 1.003µ

Fixed flange = 1.098µ

End flange = 1.002µ

Each 11th. Layer of collar sheets high permeability.