Cn (mT@12.5A)                3.751          3.750           3.754

# Mean value along the length of the aperture :  µ = 1.002

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 130 = 1.002µ

Fixed flange = 1.076µ

End flange = 1.083µ