Cn (mT@12.5A)                3.754          3.753           3.755

# Mean value along the length of the aperture :  µ = 1.002

Protection sheets permeability = 1.007 – 1.013 µ (limit max. 1.02µ)

Pole pieces charge 128 = 1.002µ

Fixed flange = 1.103µ

End flange = 1.017µ